## Slide 1: Journal club presentation
S. Karimi
Dr. Farsinejad
Nov.2021

## Slide 3: Introduction
Electrospun nanofibers
Wound dressings
Properties of nanofiber-based dressings for wound healing
Carboxymethyl kappa-carrageenan (CMKC) + polyvinyl alcohol (PVA)

## Slide 4: Mterials & Methods
CMKC + PVA
Carboxymethylation of kappa-carrageenan
Electrospinning of PVA-CMKC nanofibers
Characterization of PVA-CMKC nanofibers

## Slide 5: Mterials & Methods
Antibacterial activity: Bacteria adhesion and morphology on the nanofibers
Hemostatic activity : Protein adsorption on the nanofibers
Platelet adhesion and activation
Whole blood clotting

## Slide 6: Results
Characterization of PVA/CMKC nanofibers
 | % C1s | % N1s | % O1s | % S2p
PVA | 70.53 | 0.00 | 29.47 | 0.00
PVA-CMKC 25% | 66.78 | 0.00 | 32.79 | 0.43
PVA-CMKC 50% | 60.99 | 0.00 | 38.50 | 0.51
PVA-CMKC 75% | 65.15 | 0.00 | 34.18 | 0.67

## Slide 7: Nitrogen content of the nanofibers before and after protein adsorption experiments, obtained from XPS survey scans.
% N (before) | % N (fibrinogen) | % N (albumin) | 
PVA | 0.00 | 5.28 | 3.03
PVA-CMKC 25% | 0.00 | 3.38 | 1.83
PVA-CMKC 50% | 0.00 | 4.69 | 0.17
PVA-CMKC 75% | 0.00 | 3.13 | 0.61

## Slide 8: Results

## Slide 9: Results
Hemostatic activity

## Slide 10: Results
SEM micrographs of adhered platelets
SEM micrographs of adhered platelets

## Slide 11: Results
Whole blood clotting

## Slide 12: Results
Bacteria adhesion on the nanofibers

## Slide 13: Results

## Slide 14: Results SEM images of S. aureus on the nanofibers after 24 h of incubation

## Slide 15: Results SEM images of P. aeruginosa on the nanofibers after 24 h of incubation.

## Slide 16: Conclusion
PVA-CMKC nanofibers